Mechanical Behaviour of High Strength Concretes with High-Volume Fly Ash

Sengul, O., Tasdemir, C., Yüceer, Z., Erbaydar, M., Tasdemir, M.A.

ABSTRACT

Eight concrete mixes were prepared using the same Portland cement (OPC) and the same type of low-lime ground fly ash, in which the aggregate grading of concrete, water-binder ratio, and the maximum particle size of aggregate were kept constant, but the partial replacement of cement by fly ash was varied from 0 % (OPC concrete) to 70 %, in steps of 10 %. The replacement was on one to one weight basis. At 28 days, however, there was little reduction in compressive strength up to 40 % cement replacement by ground fly ash; then significant decrease was recorded for the further fly ash dosages. The 56-day compressive strength up to 40 % cement replacement by fly ash is almost identical to that of the no fly ash concrete. Beyond this level, the compressive strength decreases significantly. It is also shown that the brittleness index increases substantially with increasing compressive strength of concrete. The mortar phases of these concretes were also prepared.  The results obtained show that, for the mortar phases, when the dosage of fly ash increases, 2-, 7-, and 28-day compressive strengths decrease. The 56-day compressive strength of mortar, however, up to 40 % cement replacement by ground fly ash was nearly equal to that of no fly ash mortar.

# Introduction

Fly ash is a by-product of the combustion of pulverized coal in thermal power plants.  It is removed by the dust collection system as a fine particulate residue from the combustion gases before discharging into atmosphere [1,2]. The structures, compositions and properties of fly ash particles depend on the structure and composition of the coal and the combustion process by which fly ash is formed. Fly ashes exhibit pozzolanic activity in concrete. They include meta-stable alumino-silicates that will react with calcium ions, in the presence of moisture, to form calcium silicate hydrates [2,3]. The fly ash production in the world is approximately 450 million tons per year. Only about 6 percent of the total available fly ash is used as an artificial pozzolan in blended Portland cements or in concrete mixtures [4]. There are eleven active coal-burning power plants in Turkey. The annual fly ash production in the country is about 15 million tons, however, its utilization is less than the expected consumption. There are two reasons for this: i) insufficient data on the properties of the fly ashes, and ii) non-uniformity of their properties [5].

There are two major reasons to use fly ash in concrete; i) economy and ii) fresh and hardened concrete properties. The economical use of fly ashes depends on the quantity available, the amount of transportation required, the extend of beneficiation, and the design of requirement. Fly ash reduces heat of hydration, and because of spherical particles, it improves the stability of fresh concrete leading to easy mixing and placing [2,3]. There is a growing interest in the use of high performance concrete, which provides overall durability and high strength [6]. The utilization of fly ash as a partial replacement of cement has important economical, environmental, and technical benefits such as reduced waste materials, cleaner environment, reduced energy requirement, durable service performance during the service life and cost-effective structures [4,7,8].

Recent advances indicate that the design of concrete structures should be based on the principle “Strength through Durability” rather than “Durability through Strength” [7]. There have been many published reports on the microstructure, production, durability and mechanical properties of high strength concrete using superplasticizers and mineral admixtures such as fly ash, ground granulated blast-furnace slag and silica fume. Chemical composition, particle size distribution, fineness, and pozzolanic activity of fly ash, and curing conditions of concrete are important factors affecting the mechanical properties of fly ash concrete [3,9-11].

In recent years, it has been shown that the filler effect of mineral admixtures may be as important as their pozzolanic effects; according to some researchers, however, the filler effect is more important than the pozzolanic effect [8,12-14]. Particle size distribution clearly plays a very important role in the rate of chemical reactivity and in the water demand [15]. According to ASTM C 618, fly ash can be divided into two categories: Class F and Class C. The Class F ash is produced from combustion of anthracite and bituminous coals which is low lime fly ash and mainly classified as pozzolans. The Class C ash, however, is produced from combustion of either lignite or subbituminous coal.  Due to high calcium content the Class C ashes possess substantial cementitious properties besides pozzolanic properties [16,17]. Pozzolanic reaction takes place on the surface of the particles, thus, increasing surface area of fly ash has an important effect on pozzolanic activity. Thus, the fineness of the fly ash is very important for the modification of cement paste-aggregate interfacial zone, which is the weakest link in concrete. In a recent investigation done by the research group of this study [18], a coarse F type fly ash with a Blaine surface area of 222 m2/kg was ground to four different finenesses such as 337, 450, 538 and 604 m2/kg. The purpose of the work mentioned was to study how grinding of a fly ash affects its physical properties, and how the fineness of fly ash influences the strength development of both standard cement mortar and concrete. The aim of this work presented here, however, is to investigate the amount of finely ground fly ash (i.e. 604 m2/kg) on the mechanical behaviour of high and normal strength concretes.

# Experimental Studies

## Materials

The fly ash used in this study was brought from Catalagzi power plant, which is located in the west coast region of Black Sea in Turkey. The Portland cement used (OPC 42.5) is a production of Akcansa Cement Factory in Buyukcekmece-Istanbul.   7- and 28-day compressive strengths of the standard RILEM-Cembureau cement mortars are 45.8 MPa and 57.3 MPa, respectively. Compositions of OPC and fly ash are shown in Table 1.

Table 1. Chemical compositions of OPC and fly ash

| Oxide Composition (%) | OPC | Fly Ash |
| --- | --- | --- |
| SiO2 | 20.0 | 60.2 |
| Fe2O3 | 3.6 | 6.7 |
| Al2O3 | 5.1 | 21.8 |
| CaO | 63.2 | 2.5 |
| MgO | 1.1 | 1.6 |
| SO3 | 2.8 | 0.5 |
| K2O | 0.8 | 4.9 |
| Na2O | 0.3 | 0.5 |
| Cl- | 0.03 | 0.006 |
| Loss on ignition | 2.8 | 0.3 |

The average particle size of the fly ash used is relatively fine and characterized by a high density. Some physical properties of fly ash are shown in Table 2. In this study, only the ground fly ash indicated in Table 2 was used.

Table 2. Some physical properties of fly ash

| Property | Fly Ash |  |
| --- | --- | --- |
|  | Before grinding | After grinding |
| Density | 2.00 | 2.51 |
| Blaine surface area, m2/kg | 222 | 604 |
| Retained on 200 m sieve, % | 12.0 | 0.0 |
| Retained on 90 m sieve, % | 33.0 | 0.7 |
| Retained on 45 m sieve, % | 50.0 | 3.7 |

The test results obtained by the authors of this study show that [18], the physical properties such as density and fineness change as the fly ash is ground. The physical changes due to grinding are: i) the fineness of fly ash increases, ii) there is a remarkable increase in density by reducing the porosity of the fly ash particles, iii) the spherical fly ash particles transform into the mostly irregular shapes; some small fly ash particles keep their original shapes. The setting times of cement paste with fly ash were determined using Vicat needle. As seen in Figure 1 the setting times of the paste are prolonged with increasing fly ash content in the paste. Similar results were obtained in references 15 and 18.

Fig. 1.  Setting times versus fly ash contents in the paste

As seen in Figure 2, particle size distributions were also obtained in reference 18.  Figure 2 shows that the average particle size decreases by grinding of the coarse fly ash. Details regarding the fineness of fly ash are given in reference 18.

Particle Diameter, µm

Cumulative percentage

0

50

100

1.0

10.0

100.0

1000.0

After grinding

Before grinding

25

75

Fig. 2.  Particle size distributions of fly ashes before and after grinding

The requirements of ASTM C 618 [16] are given in Table 3 together with those of   EN 450 [19]. The test results of the fly ash used are given in the last column of the table. Here, S: SiO2, A: Al2O3, and F: Fe2O3

Table 3. Specification requirements of EN 450 and ASTM C 618 for fly ashes [16,19]

|  | EN 450 | ASTM C 618 |  | Fly Ash used |
| --- | --- | --- | --- | --- |
|  |  | Class F | Class C |  |
| S + A + F, min. % | 70.0 | 70.0 | 50.0 | 88.6 |
| SO3 , max. % | 3.0 | 5.0 | 5.0 | 0.5 |
| Moisture content, max. % | 3.0 | 3.0 | 3.0 | 0.1 |
| LOI, max. % | 5.0 | 6.0 | 6.0 | 0.4 |
| Available alkalis, as Na2O max. % | - | 1.5 | 1.5 | 0.3 |
| Amount retained when wet-sieved on No.325 (45m) sieve, max. % | 40.0 | 34.0 | 34.0 | 3.7 |

As seen in Table 3, EN 450 and ASTM C 618 Class F limit the minimum amount of S+A+F to 70%. ASTM C 618 Class C, however, limits the S+A+F to 50%.  According to ASTM C 618 which classifies fly ashes based on their S+A+F contents and the parent coal from which they are obtained, only one of the fly ashes produced in the eleven thermal power plants in Turkey satisfies Class F, which is produced in Catalagzi, and it was used in this work. The others, however, are obtained from lignite or sub-bituminous coal [5]. The amount of S+A+F in the fly ash used satisfies these standard specifications. BS 3892 [20] limits the maximum amount of the loss on ignition (LOI) to 7 %. The specification requirements of EN 450 and BS 3892 for SO3 are less than that of ASTM C 618. The fly ash used in this study, however, satisfies the maximum values for SO3 indicated in these standards.

## Pozzolanic Activity

Pozzolanic activity is the most critical property of the fly ash. There are different methods for the determination of the pozzolanic activity index of fly ashes. For the fly ash used in this study, the pozzolanic activity test with lime was done according to ASTM C 311-85 [21]. The test results obtained are given in Table 4 together           with ASTM C 618-85 [16]. An increase in the fineness of the same fly ash used in reference 18 leads to a substantial increase in its activity index at 7 days. As seen in this table increasing the Blaine surface area from 222 m2/kg to 604 m2/kg has resulted in an increase of 79.7 % in corresponding compressive strengths at 7 days.

Table 4. Results of pozzolanic activity index test

| Compressive strength at 7 days, MPa | Fly ash |  |
| --- | --- | --- |
|  | Before grinding, Blaine S.A.: 222m2/kg | After grinding, Blaine S.A.: 604m2/kg |
| Experiment | 7.9 | 14.2 |
| Class F in ASTM C618-85, min. | 5.5 | 5.5 |

## Mix Design

Eight concrete mixes were prepared using the same Portland cement (OPC) and the same type of low-lime ground fly ash (Class F in ASTM C 618), in which the aggregate grading, water-binder ratio, and the maximum particle size of aggregate were kept constant, but the partial replacement of cement by fly ash was varied from 0 % (OPC concrete) to 70 %, in steps of 10 %. Partial replacement of cement by fly ash was on one to one weight basis.  The grading curve of concrete aggregate was chosen between ISO A16-B16 and closer to B16. Concrete mixes produced had a water-binder ratio    of 0.35. A superplasticizer was used to maintain approximately the same slump          of   100  20 mm.

The concrete mixes were designated with the following codes: NC, FAC 00, FAC 10, FAC 20, FAC 30, FAC 40, FAC 50, FAC 60, and FAC 70. Concretes without and with fly ash were named NC and FAC, respectively. The number following FAC shows the partial replacement of cement by fly ash, which varies from 0 % (NC) to 70 %      (FAC 70). All mixes were prepared in a small laboratory mixer with vertical rotation axis by forced mixing. Details of the mixes are shown in Table 5.

Table 5. Mix proportions and some properties of fresh concretes

| Mix Code | NC | FAC 10 | FAC 20 | FAC 30 | FAC 40 | FAC 50 | FAC 60 | FAC 70 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cement (C), kg/m3 | 472 | 424 | 375 | 330 | 283 | 237 | 189 | 142 |
| Fly Ash (FA), kg/m3 | 0 | 47 | 94 | 141 | 189 | 237 | 284 | 330 |
| Water (W), kg/m3 | 166 | 165 | 164 | 165 | 165 | 165 | 165 | 165 |
| Superplasticizer, kg/m3 | 2.6 | 2.1 | 2.3 | 2.4 | 2.5 | 2.5 | 2.5 | 2.5 |
| Sand (0-2 mm), kg/m3 | 260 | 259 | 256 | 256 | 255 | 254 | 252 | 249 |
| Basalt fines, (0-4 mm), kg/m3 | 475 | 472 | 467 | 466 | 465 | 463 | 460 | 456 |
| Crushed basalt No. I, (4-16 mm) kg/m3 | 1121 | 1114 | 1101 | 1100 | 1096 | 1092 | 1084 | 1074 |
| Air, % | 2.2 | 2.2 | 2.8 | 2.3 | 2.1 | 1.8 | 1.9 | 2.2 |
| Slump, mm | 110 | 90 | 105 | 105 | 110 | 100 | 95 | 110 |
| W/(C+FA) | 0.35 | 0.35 | 0.35 | 0.35 | 0.35 | 0.35 | 0.35 | 0.35 |
| Unit weight, kg/m3 | 2496 | 2483 | 2459 | 2460 | 2455 | 2450 | 2436 | 2418 |

Mortar phase of each concrete was also produced. In the preparation of these mixes; water, cement, fly ash, sand, and basalt fines were in the mortar phase. Table 6 shows mix compositions and some properties of fresh mortars. The mortar mixes               were designated with the following codes: NM, FAM 10, FAM 20, FAM 30, FAM 40, FAM 50, FAM 60, and FAM 70. Mortars without and with fly ash were named NM and FAM, respectively; the number following FAM shows the partial replacement of cement by fly ash, which varies from 0 % (NM) to 70 % (FAM 70). The beams prepared for the standard RILEM-Cembureau tests were 160 mm in length and          40 mm x 40 mm in cross-section. All specimens were demolded after 24 hours, stored in water tank saturated with lime at 20oC until the testing day. After the bending tests, the compressive tests were performed on the half beams using 40 mm x 40 mm    cross-section.

Table 6. Mix compositions and some properties of fresh mortars

| Mix Code | NM | FAM 10 | FAM 20 | FAM 30 | FAM 40 | FAM 50 | FAM 60 | FAM 70 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Cement (C), kg/m3 | 804 | 722 | 639 | 557 | 477 | 395 | 314 | 234 |
| Fly Ash (FA), kg/m3 | 0 | 79 | 160 | 238 | 317 | 395 | 470 | 545 |
| Water (W), kg/m3 | 281 | 280 | 280 | 278 | 278 | 271 | 274 | 273 |
| Sand, (0-2 mm), kg/m3 | 444 | 441 | 436 | 432 | 428 | 423 | 417 | 411 |
| Basalt fines, (0-4mm), kg/m3 | 809 | 803 | 796 | 787 | 781 | 772 | 762 | 753 |
| W/(C+FA) | 0.35 | 0.35 | 0.35 | 0.35 | 0.35 | 0.34 | 0.35 | 0.35 |
| Air, % | 0.9 | 0.7 | 0.5 | 0.6 | 0.4 | 1.0 | 0.9 | 1.0 |
| Spread, % | 72 | 62 | 68 | 60 | 62 | 65 | 54 | 47 |
| Unit weight, kg/m3 | 2337 | 2325 | 2311 | 2293 | 2280 | 2256 | 2237 | 2216 |

## Test Procedure

Three 150 mm cubes were used for the standard compressive strengths of concretes.  Strength tests of mortars, however, were done in accordance with the RILEM-Cembureau Method. For the determination of modulus of elasticity and hystereris loops, at least three cylinders of 150 mm diameter and 300 mm height were prepared. Compressive strengths of concretes with and without fly ash were determined at 28 and 56 days.  The tests of the brittleness index and modulus of elasticity were done at 56 days.  Strength tests of mortars were determined at 2, 7, 28, and 56 days.  Mechanical test results are given in Table 7 and 8.

Table 7. Mechanical properties of concretes

| Mix Code | Cube compressive strength of concrete, MPa |  | Modulus of elasticity at 56 days, MPa | Brittleness Index at 56 days |
| --- | --- | --- | --- | --- |
|  | 28 days | 56 days |  |  |
| NC | 82.8 | 92.1 | 47300 | 3.60 |
| FAC 10 | 70.2 | 87.5 | 47400 | 3.47 |
| FAC 20 | 60.2 | 90.9 | 49300 | 3.26 |
| FAC 30 | 66.0 | 93.0 | 47800 | 3.63 |
| FAC 40 | 66.1 | 84.7 | 47500 | 3.32 |
| FAC 50 | 58.5 | 74.6 | 46200 | 2.90 |
| FAC 60 | 43.4 | 64.3 | 44600 | 2.27 |
| FAC 70 | 34.1 | 49.3 | 40100 | 1.75 |

Table 8. Compressive strengths of mortars

| Mix Code | Compressive strength of mortar, MPa |  |  |  |
| --- | --- | --- | --- | --- |
|  | 2 days | 7 days | 28 days | 56 days |
| NM | 48.3 | 80.8 | 97.3 | 103.8 |
| FAM 10 | 43.3 | 75.3 | 97.1 | 105.6 |
| FAM 20 | 38.0 | 67.1 | 91.7 | 103.1 |
| FAM 30 | 33.3 | 58.5 | 92.1 | 102.8 |
| FAM 40 | 25.9 | 51.0 | 85.2 | 101.6 |
| FAM 50 | 18.3 | 43.3 | 74.4 | 92.7 |
| FAM 60 | 14.0 | 34.3 | 64.8 | 75.4 |
| FAM 70 | 7.3 | 21.9 | 46.1 | 56.9 |

## Modulus of Elasticity and the Brittleness Index

The elastic moduli were calculated from the stress-strain curve for stresses below approximately 30 percent of the ultimate strength and the results obtained are given in Table 7. The Brittleness Index B, obtained from the loading-unloading curve for each concrete with and without fly ash in compression, is defined as the ratio of the elastic deformation energy to the irreversible deformation energy corresponding to the       pre-peak point of the stress-strain curve.

As shown in Figure 3, Brittleness Index B may be expressed as the ratio of area SII to area SI, where SI is the irreversible deformation energy due to damage and SII is the elastic (reversible) deformation energy. When the ratio of SII/SI approaches zero, all energies become irreversible; when it tends to infinity, all energies become reversible. Thus, an increase in B indicates increased brittleness. Table 7 summarizes the test results obtained for all concretes tested.

Deformation

Stress

Fig. 3.  Definition of reversible and irreversible energies

# Results and Discussion

## Compressive Strengths of Concretes

As seen in Table 7 and Figure 4, in general, compressive strengths increase with the age of concrete and decrease with the amount of fly ash. The compressive strengths obtained in this study were in excess of 34 MPa at 28 days even at 70 % replacement of cement by a ground fly ash; such a fly ash concrete can be considered as a structural concrete. For concretes up to 70 % cement replacement by fly ash and 28-day age, the fly ash concretes show slightly lower strengths compared to no fly ash concrete. The 56-day compressive strength becomes stable up to 40 % ground fly ash replacement. Beyond this level, since the amount of fly ash used is relatively high, it has insufficient binding value and causes reduction in both 28- and 56-day compressive strengths.  The results obtained shows that the rate of strength gain in concretes with fly ash is significant between 28 and 56 days. It can be concluded that high strength concrete could be made with 40 % cement replacement by finely ground fly ash.

## Compressive Strengths of Mortar Phases

As seen in Table 8 and Figure 5, as the dosage of fly ash increases, the 2, 7, and 28-day compressive strengths decrease. As seen in figure at 56 days the compressive strength of mortar phase of concrete, up to 40 % cement replacement by ground fly ash becomes stable and almost the same. Beyond this level, compressive strengths of both concretes and their mortar phases decrease significantly. The rate of strength gain in fly ash concretes is substantial. Thus, it can be concluded that mortar made with low cement content and high volumes of ground low lime calcium fly ash exhibits relatively low strengths at early ages, but higher strengths at later ages.

28 days

56 days

Fig. 4.  Compressive strengths of concretes at 28 and 56 days

Fig. 5.  Compressive strengths of mortar phases at 2, 7, 28 and 56 days

## The Brittleness Index

Figure 6 shows the brittleness index versus compressive strength plot in concretes with and without fly ash at 56 days. The circles indicated in the figure show individual test results obtained from the brittleness index test, but the data given in last column of Table 7 shows the average values. As seen in this figure, substantial increase in the brittleness index is typical for high strength concretes. At HSCs, the interface becomes more homogeneous and dense; as a result bond strength increases. The stress-strain relation in these concretes is almost linear up to a stress as high as 90 % of the ultimate strength and the loop obtained becomes narrower. Thus, in these concretes the irreversible deformation energy decreases and the material becomes more brittle.   Similar results were obtained in some previous works [22-25].

Fig. 6.  Brittleness index versus compressive strengths at 56 days

# Conclusions

Following conclusions could be drawn from the results obtained in this study.

- Compressive strength of concrete increases with age, but decreases with inclusion of fly ash. Similar trends are obtained for the mortar phases of concretes with fly ash.

- For concretes up to 40 % cement replacement by ground fly ash and 28-day age, the fly ash concretes show slightly lower strengths compared to the concrete without fly ash. Beyond this level, compressive strength decreases significantly. The compressive strengths obtained in this work, however, were in excess of 34 MPa at 28 days even at 70 % cement replacement by finely ground fly ash.

- The experimental results obtained in this work show that the finely ground fly ash percentage can be used up to 40 % of total cementitious material in order to produce high strength concrete.

- The concretes with fly ash show significant increases in compressive strength at 56 days. The 56-day compressive strength up to 40 % cement replacement by ground fly ash is almost identical to that of the concrete without fly ash. Beyond this level, there is substantial decrease in strength.

- In high strength concretes, the brittleness index increases significantly with increasing compressive strength. The brittleness index can be used as an indication of the brittleness in concrete.

- For both concretes and their mortar phases, the rate of strength gain is lower for mixtures containing fly ash, at early ages. Beyond 28-day age, the rate of strength gain in concretes (or in their mortar phases) with fly ash is significant between 28- and 56-days.

- The modulus of elasticity of concretes up to 50 % cement replacement by ground fly ash is almost constant, and then it decreases slightly with fly ash content.

Acknowledgement

This research was completed at Istanbul Technical University. Some physical and chemical tests on fly ash were made at Akcansa Cement Industry and Trading Company – Betonsa Technological Center.

# References

- Joshi, R.C., “Critical Review on Production, Properties, and Utilization of Fly Ash in Concrete”, in Shigeyoshi Nagataki Symposium on Vision of Concrete: 21 st Century, CANMET, Ottowa, 1998, pp.141-155.

- Berry, E.E., and Malhotra, V.M., “Fly Ash in Concrete”, in Supplementary Materials in Concrete, Chapter 2, V.M. Malhotra (ed.), CANMET, 1987,  pp.37-163.

- Atac, A., Tasdemir, C., Sonmez, R., and Tasdemir, M.A., “Effects of Curing Conditions on Strength and Permeability Properties of Concretes with Various Fly Ash Contents”, fib-Symposium on Concrete and Environment, Berlin, 3-5 October, 2001, 14 pp.

- Mehta, P.K., “Reflections on Recent Advancements in Concrete Technology”, in Second International Symposium on Cement and Concrete Technology in the 2000s, 6-10 September 2000, Istanbul, Vol.1, pp.43-57.

- Tokyay, M., “Characterization of Turkish Fly Ashes”, Turkish Cement Manufacturers Associations, Ankara, 1998.

- Tasdemir, M.A., Tasdemir, C., Akyüz, S., Jefferson, A.D., Lydon, F.D., and Barr, B.I.G., “Evaluation of Strains at Peak Stresses in Concrete: A Three-Phase Composite Model Approach”, Cement and Concrete Research, Vol.20, 1998, pp. 301-318.

- Swamy, R.N., “Holistic Design of Concrete Technology: The Only Route to Durability and Sustainability in Construction”, in Second International Symposium on Cement and Concrete Technology in the 2000s, 6-10 September 2000, Istanbul, Vol.1, pp.58-72.

- Goldman. A., and Bentur, A., “The Influence of Microfiller on Enhancement of Concrete Strength ”, Cement and Concrete Research, Vol.23, 1993, pp.962-972.

- Monzo, J., Paya, J., and Peris-Mora, E., “A Preliminary Study of Fly Ash Granulometric Influence on Mortar Strength”, Cement and Concrete Research, Vol.24, No.4, 1994, pp.791-796.

- Paya, J., Monzo, J., Borrachero, M.V., Peris, E. and Gonzalez-Lopez, E., “Mechanical Treatments of Fly Ashes. Part III: Studies on Strength Development of Ground Fly Ashes-Cement Mortars”, Cement and Concrete Research, Vol.27, No.9, 1997, pp.1365-1377.

- Kiattikomol, K., Jaturapitakkul, C., Songpiriyakij, S. and Chutubtim, S.,         “A Study of Ground Coarse Fly Ashes with Different Finenesses from Various Sources as Pozzolanic Materials”, Cement and Concrete Composies, Vol.23, 2001, pp.335-343.

- Tasdemir, C, Tasdemir, M.A., Lydon, F.D., and Barr, B.I.G. “Effects of Silica Fume and Aggregate Size on the Brittleness of Concrete”, Cement and Concrete Research, Vol.26, No.1, 1996, pp.63-68.

- Tasdemir, C., Tasdemir, M.A., Grimm, R., and Konig, G., “Microstructural Effects on the Brittleness of High Strength Concretes”, in Fracture Mechanics of Concrete Structures, Proc. FraMCoS-2, F.H. Wittmann, (ed.), Aedificatio Publishers, Freiburg, Germany, 1995, Vol.1, pp.125-134.

- Tasdemir, C, Tasdemir, M.A., Mills, N., Barr, B.I.G., and Lydon, F.D., “Combined Effects of Silica Fume, Aggregate Type and Size on Postpeak Response of Concrete in Bending ”, ACI Materials Journal, Jan-Feb. 1999, pp.74-83.

- Cheng, H.Q., and Osbaek, B., “Effects of Fly Ash Grinding on the Hydration and Strength Development of Fly Ash Cements” The 8th International Congress on the Chemistry of Cement, September 22-27, 1986, Rio de Janerio, 7 pp.

- ASTM, “Standard Specifications for Fly Ash and Raw or Calcined Natural Pozzolan for Use as Mineral Admixture in Portland Cement Concrete ”, ASTM, Philadelphia, ASTM C 618-85, 1985.

- Naik, T.R., Singh, S.S., and Hu, W.Y., “High Volume Fly Ash Concrete Technology”, Research Project No. 3176-1, The University of Wisconsin-Milwaukee, Center for By-Products Utilization, 1992.

- Demir, M., Erenoglu, T., Ekim, H., and Tasdemir, M.A., “Effects of Fineness and Amount of Fly Ash on Strength Development of Concrete”, to be submitted at the Fifth International Congress on Advances in Civil Engineering          (ACE 2002), September 25-27, 2002, Istanbul.

- EN 450, “Fly Ash for Concrete”, CEN, Brussels, 1994.

- BSI, “Specifications for Pulverized Fuel Ash for Use as a Cementitious Component in Structural Concrete”, BSI, London, BS 3892, Part 2, 1982.

- ASTM, “Standard Methods of Sampling and Testing Fly Ash or Natural Pozzolans for Use as a Mineral Admixture in Portland Cement Concrete”, ASTM, Philadelphia, ASTM C 311-85, 1985.

- Tasdemir, C., “Effects of Aggregate-Cement Paste Interface Microstructure on Fracture Parameters of HSCs”, PhD Thesis, Istanbul Technical University, 1995. (in Turkish with English Summary).

- Tasdemir, C., Sarkar, S.L., Tasdemir, M.A., Akyüz, S.,and Koca, C., “Effect of Silica Fume on the Brittleness of HSCs under Compression”, proc. ERMCO 95, 1995, pp.444-452.

- Tasdemir, M.A., Tasdemir, C., Ozbek, E., and Altay, B., “Fineness Effect of GGBS on the Properties and Microstructure of Concrete”, First International Symposium on Mineral Admixtures in Cement, 6-9 November 1997, Istanbul, TCMA, pp.198-215.

- Sengul, O., Tasdemir, C., Tasdemir, M.A., Hacikamiloglu, M., Ozbek, E., and Altay, B. “Effects of Aggregate Type on the Mechanical Properties of Normal and High Strength Concretes”, Second International Symposium on Cement and Concrete Technology in the 2000s, 6-10 September 2000, Istanbul, pp.40-49.